Annex N1

Technical Requirements

Product Name

- LIME

Specifications

Richness:                                                                                         100,00            %CaO Specific mass:                                                                                   0,90              kg/l

Acceptable Specifications option 1 – preferable option:

We would like to have the 1st quality product

High CaO values.

Its particule size  should preferably be more like a 0 to 1 mm than a 0 to 3 mm

Acceptable Specifications option 2:

Description

Chemical name: calcium oxide

Chemical formula: CaO

Condition: Fine particle powder

Atomic Mass: 56.08

Known as: Lime - slaked and unslaked

Name in accordance with UNE-EN 459:	CL 90-Q

Physical characteristics

A single-component substance, calcium oxide, ერთკომპონენტიანი ნივთიერება, კალციუმის ოქსიდი, which contains a small percentage of SiO2, Al2O3, Fe2O3, MgO and CaCO3; It is a raw material of natural limestone. The natural product is obtained by calcination at 1200 ºC, approximately CaCO3.

| Appearance | white color, dry, odorless, strong hygroscopic nature |
| --- | --- |
| Crystal structure | cubic |
| PH | 12.4 saturated solution at 25ºC |
| Density | 940 gr/l |
| Boiling temp. | 2.850 ºC |
| Cooling temp. | 2.600 ºC |
| Weight | 3,34 kg/l 20 ºC |
| Solubility H2O | soluble in acid, glycerin and sucrose solutions |
| Reaction with acid | formation of calcium salts by exothermic reaction |
| Reaction with water | calcium hydroxide is produced during the reaction |

Technical data				marginal volume

CO2 					1 % 		≤ 3

Total CaO				97 % 		≥ 93

Reaction with water 60ºC 		4:00 		min ≤ 10

SiO2 					0.2 % 		≤ 0.7

Al2O3 					0.2 % 		≤ 0.3

Fe2O3					0.15 % 		≤ 0.3

Mg					O 1 % 		≤ 1.2

Combined H2O				0.1 % 		≤ 0.3

S 					0.5 %		≤ 0.6

Granulometry:

Sieving Method 5 mm 		0 %

Sieving Method 2 mm 		<12 %

USAGE

The product is used in agricultural, industrial, environment-related activities and livestock farming. For environmental pH and water hardness regulation, remineralization, metal removal, treatment plant and general drinking, industrial or sewage/waste water treatment. For gas treatment of waste fuel and thermal power stations. For soil sabilization, for preparation of construction slurry.

Lime is used for various purposes: neutralizing, melting, caustic, scouring, drying, absorbing, disinfecting, waterproofing and of course as a raw material.

Regulations

| UNE-EN 459 - part 1, 2, 3 | Limestone for construction |
| --- | --- |
| UNE 80502:2003 | Application of slaked or hydrated lime for soil improvement/stabilization |
| UNE 80503:2001 | Use of calcium hydroxide in asphalt mixtures |
| UNE-EN-12518 | In chemical products used for the treatment of water for human consumption - limestone |
| UNE-EN-12485 | In chemical products used for the treatment of water for human consumption - calcium carbonate, limestone, semi-calcined dolomite |

Chemical Abstracts Service Registry Number 1305-78-8

European Invertory of Chemical Substances 215-138-9

Special requirements for shipment - Compulsory

Delivery should be done Bulk in a specialized tanker (Silo truck incl. hydraulic discharge) from which the lime can be fed directly to SILO

Silo loading pressure is 1bar max.

Silo capacity - max. 42 m3

SILOTRUCK should by all means have all the necessary devices (pumps or air impeller) to charge our SILO.

S

Connection to SILO

Dimensions of the flange needed

Example video for SILOBUS discharging process –please download:

https://we.tl/t-Okzm8UyPmS

Real photos: