Requested positions:

- Metal Primer PR 200 REMA TIP TOP – 17.25 kg

- High-strength lining REMALINE 50/CN, thickness (S-10 mm) – 110,55  m²

Specification:

- Wear resistance against wet abrasive abrasion;

- Protection against material sticking;

- Tensile strength;

- High cut resistance;

- Presence of a bonding (adhesive) layer compatible with CEMENT SC 4000;

- Polymer base NR according to DIN ISO 1629;

- Specific gravity within 1.11 g/cm³;

- Shore A hardness of approximately 51 units;

- Mass of approximately 11.70 kg/m².